RAKU GLAZES AND SLIPS AVAILABLE  All glazes are made to apply by brush using underglaze medium/water 50/50

| Glaze/slip | Constituents per litre | Notes |
| --- | --- | --- |
| - Red | CTM red glaze 1000 | Needs two good coats. Can be unreliable |
| - Yellow | CTM yellow glaze 1000 | Needs two good coats. Can be unreliable |
| - White Dave Roberts | Calcium borate frit 400 Borax frit 400 China clay 150 Tin oxide 50 | Best with two coats. |
| - Turquoise/copper | CTM turquoise 1000 | Two coats. Gives attractive copper patches in heavy reduction |
| - Dark Green | Borax frit 500 High Alkali Frit 500 China clay 30 Copper carbonate 90 | Two coats recommended. Attractive dark green. Some copper flashes in heavy reduction. |
| - Dark blue/copper “Blue Gold” | High alkali frit 900 China clay 50 Tin oxide 40 Bentonite 10 Copper oxide 30 | Two coats. Dark blue. Good copper flashing in reduction. Can pinhole. |
| - Susan Luker clear/white on white clays. [Sacrificial glaze for naked raku] | Borax frit 450 High alkali frit 450 China clay 80 Bentonite 10 | Two coats if using as a straight glaze. Good reliable clear/white crackle. I use it mainly as the sacrificial glaze for naked raku. If using it for this apply one thick coat over dried resist slip [below] and dry before firing to 900 degrees C. |
| - Resist slip for naked raku | China Clay 600 Flint 400 Alumina 50 | Apply one thick coat to burnished and biscuited pot. Ensure the whole surface is fully covered. Dry and then cover with sacrificial glaze as above. |